## Slide 1: Recycling Polylactic Acid
The 3 Rs and the Products of the Future

## Slide 2: Recycling Polylactic Acid
Experiment:
Step 1

## Slide 3: Step 1
Safety first: put on a lab coat, protective goggles and gloves.

## Slide 4: Step 1
Cut the PLA cup into small pieces using scissors. The smaller the pieces are, the faster the reaction will be.
Place the PLA pieces into a weighing boat.
Measure 5 g of PLA pieces on a digital scale.

## Slide 5: Step 1
Add 5 g of PLA pieces into the 250 mL Erlenmeyer flask using a funnel.

## Slide 6: Step 1
Using the graduated cylinder, measure 100 mL of the pre-prepared solution (1.4 M NaOH in 1:1 ethanol/water).
Add the solution and 1 magnetic stirring rod into the flask.

## Slide 7: Step 1
Place the flask onto the hot plate.
Turn on the heating function of the hot plate and heat the solution to 90˚C (reduce the heat if the flask begins to boil vigorously).

## Slide 8: Step 1
Heat and stir the solution with a stirring rod until the PLA pieces have completely dissolved.

## Slide 9: Step 1
After the PLA pieces have completely dissolved and the solution is pale yellow, turn off the hot plate. The temperature should be 80˚C – 90˚C.

## Slide 10: Recycling Polylactic Acid
Experiment:
Step 2

## Slide 11: Step 2
Use heat resistant gloves to remove flask from hot plate.
Place the flask in an ice water bath and allow the solution to cool until it is below 60˚C. This mixture is now called “hydrolysed PLA”.

## Slide 12: Recycling Polylactic Acid
Experiment:
Step 3

## Slide 13: Step 3
Using the plastic pipette, transfer 1-2 drops of the solution to the watch glass.
Test the pH of the hydrolyzed PLA by dipping a pH strip in the watch glass.
This means that the pH of the solution is 14.

## Slide 14: Step 3
Slowly add 200 drops of 6 M HCl into the flask and mix.

## Slide 15: Step 3
Measure the final pH of the solution using a pH strip. Aim for a pH range of 4-5. The solution now contains lactic acid and sodium chloride (NaCl).
pH before: 14
pH after: 5

## Slide 16: Step 3
Using a funnel, transfer the lactic acid solution into the plastic bottle. It is now ready to use.